Comments on the mechanism of aging of ATO based electrochromic displays

Joo C. Chan, Nicole A. Hannah, Shankar B. Rananavarea)

Department of Chemistry, Portland State University, Portland, Oregon 97207

,J. P. Coleman, L. Yeager, A. Sarswat, P. Iyer,

Avery Research Center, Avery Dennison, Pasadena, California 91107

(Received

Non-stoichiometric SnOX is a rare transparent semiconductor exhibiting a large band-gap (3.6eV) and high carrier density (1019-1021cm3).[1]. Thin films of SnOx have been used in applications ranging from electrodes in LCD devices, solar cells to sensors [2]. Unlike the widely studied WO3 based electrochromic materials[3], the intrinsic electrochromic properties of SnOx are weak but can be improved by antimony doping with an optimum doping level at 40 mole % of Sb[4]. The doping leads to conductivity enhancement (n-type) by creating delocalized donor atom states near the conduction band. However, the conductivity decreases precipitously at high levels of Sb doping [5] (5%>), which can be attributed to grain boundary effects, phase separation[6], and charge transfer complexes [7,8].  ATO nanoparticles (4-9 nm) are readily synthesized by sol-gel techniques and upon calcination at 600°C they transform to a casserite crystal structure characteristic of undoped SnOx. Materials and device optimization for flexible and inexpensive displays exploiting novel in-plane anode-cathode configurations have been elucidated in a series of papers [4]. These electrochromic (EC) devices exhibit remarkable (1) memory effect (refresh times~2-24hours) (2) low power consumption (needing only 10-100μA/cm2@ 1-1.2 operational voltage) and (3) reasonable contrast ratios (2-4).

Briefly, the EC devices were constructed on flexible plastic substrates. Screen-printing anodic and cathodic areas, separated by plastic insulation, was achieved by successive deposition of silver paint, carbon ink (to prevent corrosion of Ag), TiO2 (highly conductive and reflective particles) followed by an electrochromic layer of ATO nanoparticles (dispersed in fluoroelastomer), total electro-active layer thickness ≈ 50m. The electrolyte was 30% LiCl (in water for test purposes) in a polymeric gel encapsulated in PET over layer (see Figure 1). Upon application of DC voltage, the anodic area becomes transparent due to carrier depletion and appears white due to light reflection from the underlying TiO2 layer. In the cathodic region, injection of electrons and migration of Li ions in the electrochromic layer increases its optical absorption and it appears black [6-8].

This paper examines factors affecting the device lifetime/aging, specifically the origins of distinct yellowish discoloration observed in the cathodic region during operation. Discoloration increases with the operation time and the magnitude of DC voltage. Bipolar pulse driving scheme (switching anode and cathode polarities) reduces the extent of yellowing (~1/υ). Given the mixed valence nature of both Sn+4/+2 and Sb+5/+3 oxides, the development of their colored charge transfer complexes was probed using Sn Mössbauer [9] and Sb X-ray absorption near edge structure (XANES) spectroscopies [10].  Sn spectra from yellowed regions do not show presence of peak(s) at 4-6mm/sec, characteristic of Sn+2, neither do the antimony L1 in XANE spectra reveal Sb+3 ions (Figure X).  Also, strong oxidizing (bleach) or reducing (SnCl2) solutions do not affect the discoloration. XPS studies showed no difference in elemental composition eliminating potential source due to electrolyte/polymer degradation.

Evolution of CR (~ injected charge), as the device is slowly (time≈ 3hrs.) cycled between positive and negative voltages exhibits distinct hysteresis (Figure 2a) with non-zero “remnant CR”, and a “coercing” voltage of 0.2V. Similar trapping of electrons in Si nanoparticles is well known [11].  It suggests an impeded movement of ions from electrodes, i.e., reversal of Sb(V)2O5+4e+4Li+ ↔ Li4Sb(III)2O5 reaction at cathode and vice versa at anode. To quantify, yellowing, we measured b* (CIE 1976 color coordinate) using an Ocean opticsTm reflection spectrometer, 15 minutes after shorting anode and cathode together. For fresh and yellowed samples b* values are about 2 and >4 respectively. Figure 2b shows development of b* as a function of device operation (@1.2volts) time.  b* exhibits a logarithmic growth, (b*~ logt0.5 ). While experiments involving fixed charging time and variable discharge times yielded a smaller slope of –0.3. Thus, the electrochromic process appears to be only partially reversible, controlled by very slow kinetics of charge movement.

We employed impedance spectroscopy (from 5Hz-14MHz, HP4192 LCR meter interfaced to PC) to study charge transport between electrolyte-electrode. The resulting bode plots (figure 3) were analyzed using [12] Randle’s equivalent circuit (Zsimp Version 3.2, from Princeton applied research); see table 1. Here Rs,Rp, C are the series solution resistance, the polarization resistance, and net capacitance (due electrode-electrolyte double layer and a series capacitance due to depletion layer in the semiconductor) respectively; W is the Warburg impedance becoming important on the longer time scale where diffusion and not the electron transfer rate is the rate determining step. Both Rp and Warburg impedances increase with applied potential consistent with Volmer-Butler mechanism [13]. The decrease C corresponds to increased depletion layer thickness [8].  The yellowed samples show a systematic increase in Rp, W and Rs.  The increase in Rs entails loss of mobile ions from the electrolyte qualitatively consistent with CR hysteresis. Precipitous rise in Rp and W and drastic decrease in C also suggests restructuring at nanoparticulate laden electrode-electrolyte interface due to growth of an insulating barrier.

X-ray diffraction studies of fresh and degraded devices, figure 5, indicate that upon electrochromic operation particle (grain) size decreases, especially the larger size particles.  For two devices, made from different nanoparticle size distributions, we note that particles of 4nm size undergo no further reduction in size (Table 2). These devices exhibit lesser extent of yellowing (but with lower CR). This can be understood in terms of their higher columbic charging energy (~1/size) needed for charge insertion. Chemical analysis (atomic absorption spectroscopy) of electrolyte from yellowed device contained significant amounts of Sb, table 2. Thus the mechanism can be postulated based on formation of amorphous sparingly soluble hydrated LiSbO3[12] which like NaSbO3 is a insulator, e.g. Li4Sb(III)2O5+1/2O2→

4e+2Li+4+2LiSbO3 using dissolved oxygen from electrolyte or from the SnOx lattice.  Other possibility is that insertion of Li ions is coupled to irreversible displacement of surface Sb/Sn ions, leading to p-doping and hence p-n barriers. In depletion region, color can be yellow due to lack carriers similar to color of freshly removed samples from calcination oven [7]. Li+ based p-doping in SnOx lattice using high temperature pyrolysis has been recently reported [14]. Both suggestions, are consistent with both hysteresis, kinetics of b*, electrochemical impedance and X-ray diffraction studies of the fresh and aged devices.

Acknowledgements: We wish to thank Dr. Wolfgang A. Caliebe of Brookhaven National Laboratories for collecting Sb XANE spectra on samples.

Footnotes a)To whom correspondence should be addressed. Fax: 503.725.9525, E-mail: ranavas@pdx.edu.

References

- Ç. Kýlýç and A. Zunger, Phys. Rev. Lett. 88 (9), 095501-(1-4) (2002).

- H. L. Hartnagel, A. L. Dewar, A. K. Jain, and C. Jagadish, Semiconducting Transparent thin Films, IOP Publishing Ltd, Bristol, 1995.

- For a review see, P. M. S. Monk, R. J. Mortimer, and D. R. Rosseinsky, Electrochromism: Fundamentals and Applications, (Wiley-VCH: Weinheim, Germany, 1995).

- a) J. P.Coleman and J. H. Wagenknecht, in Proceedings of the Third Symposium on Electrochromic Materials, Vol. 96 (24), p. 325 (1996). b) J. P. Coleman, A. T. Lynch, P. Madhukar, and J. H. Wagenknecht, Solar Energy Materials & Solar Cells 56 (3), 395-418 (1999); ibid. 56 (3), 375-394 (1999).

- J. C. Volta, P. Bussiere, G. Coudurier, J. M. Herman, and J. C. Vedrine, Applied Catalysis 16, 315-328 (1985).

- D. R. Pyke, R. Reid, and R. J. D. Tilley, J. Chem. Soc. Farad. Trans. I 76, 1174 (1980).

- T. Nütz and M. Haase, J. Phys. Chem. B. 104 (35), 8430-8437 (2000).

- Boschloo, G.; Fitzmaurice, D. J. Phys. Chem. B 1999, 103(16), 3093-3098.

- S. Akselrod, M. Pasternak, and S. Bukshpan, Phys. Rev. B. 11 (3), 1040-1044 (1975).

- J. Rockenberger, U. zum Felde, M. Tischer, L. Tröger, M. Haase, and H. Weller, J. Chem. Phys. 112 (9), 4296-4304 (2000).

- S. Tiwari, F. Rana, H. Hanafi, A. Hartstein, E. F. Crabbe´, Kevin Chan, Appl. Phys. Lett. 68 (10), 1377, (1996).

- C. Gabrielli, Technical Report No. 004/83, (Solartron Instruments, England, 1998).

- T. Oi, M. Endoh, M. Narimoto, and M. Hosoe, J. Mater. Sci. 35 (2), 509-513 (2000).

- M. Bagheri-Mohagheghi, M. Shokooh-Saremi, Semicond. Sci. Technol. 19 (2004) 764–769

Tables

Table 1. Electrochemical impedance analysis.

| Voltage | Re (Ω) | C (μF) | RW (Ω) | W (Ω/sec0.5) | χ2 |
| --- | --- | --- | --- | --- | --- |
| Sample 1 |  |  |  |  |  |
| 5mV (Fresh) | 13.5 | 9.1 | 0.5 | 65.5 | 8.73E-05 |
| 5mV (Yellowed) | 16.4 | 6.8 | 1.9 | 198.8 | 2.82E-04 |
| 0V (Aged Yellowed) | 278.8 | 4.5E-4 | 705.6 | 20120 | 1.29E-02 |
| Sample 2 |  |  |  |  |  |
| Fresh | 23.6 | 0.32 | 7.8 | 102.0 | 4.85E-03 |
| Yellowed | 27.1 | 0.13 | 11.8 | 408.2 | 6.62E-03 |

Table 2. Summary of experimental results for Powder X-Ray Diffraction (SnO2) and Atomic Absorption measurements for Samples 1 (old, Monsant) and 2 (new).

| Condition | Peak Position (2) Peak Width (2) Crystal Sized (nm) | Etched Material (g/cm2 Cathode (Total Electrode)) |
| --- | --- | --- |
|  |  | Peak 1 | Peak 2 | Peak 1 | Peak 2 | Peak 1 | Peak 2 | Sn | Sb |
| Sample 1 | Untreated | 26.52 ± 0.01 | 26.66 ± 0.01 | 0.11 ± 0.01 | 0.52 ± 0.02 | 41 ± 4 | 8.7 ± 0.3 | 10 (3) ± 33% | 173 (47) ± 15% |
|  | Chem. Oxidizeda | 26.54 ± 0.01 | 26.69 ± 0.01 | 0.12 ± 0.01 | 0.54 ± 0.02 | 38 ± 3 | 8.4 ± 0.3 |  |  |
|  | Oxidizedb (e) | 26.56 ± 0.01 | 26.59 ± 0.01 | 0.19 ± 0.01 | 0.99 ± 0.01 | 24 ± 1 | 4.58 ± 0.05 |  |  |
|  | Reducedc (e) | 26.55 ± 0.01 | 26.53 ± 0.01 | 0.17 ± 0.01 | 1.01 ± 0.06 | 27 ± 2 | 4.5 ± 0.3 |  |  |
| Sample 2 | Untreated | 26.57 ± 0.01 | 26.66 ± 0.01 | 0.14 ± 0.02 | 1.15 ± 0.02 | 32 ± 5 | 3.9 ± 0.1 | 0.8 (0.4) ± 500% | 70 (35) ± 20% |
|  | Chem. Oxidized | 26.55 ± 0.01 | 26.59 ± 0.01 | 0.15 ± 0.02 | 1.13 ± 0.02 | 30 ± 4 | 4.0 ± 0.1 |  |  |
|  | Oxidized (e) | 26.62 ± 0.02 | 26.63 ± 0.01 | 0.24 ± 0.04 | 1.15 ± 0.04 | 19 ± 3 | 3.9 ± 0.1 |  |  |
|  | Reduced (e) | 26.55 ± 0.01 | 26.62 ± 0.01 | 0.16 ± 0.02 | 1.12 ± 0.02 | 28 ± 4 | 4.1 ± 0.1 |  |  |

a Chemical oxidation was accomplished by coating the devices with ordinary household bleach.

b,c Electrochemical (e) oxidation and reduction was carried out by charging the devices in a LiCl bath for a period of 72 hours at 1.5 V.

d The crystal size (t) was evaluated using the Debye-Scherrer equation.

Common antimony oxides, i.e. Sb2O3 (Senamontite), SB2O4 ((-Cervantite, (-Clinocervantite, (-Cervantite), and Sb2O5, exhibit reflections at 27.7o, (25.8o, 27.7o, 27.5o) and 27.3o, respectively; hence the additional peak (at 26.6o) may originate from a distorted Casserite structure.

Figure 1. Schematic Diagram illustrating the ‘side-by-side’ design of a printed Electrochromic display

Figure X. a) Sn Mossabaur spectra from fresh (bottom) and aged(top) electrodes. b) A first derivative of XANES spectra from fresh and aged devices along with spectra from model compounds. Note that Sb2O4 is a mixture of Sb2O3 and Sb2O5.

a)							b)

Sn Mössbauer						Sb Xane Spectra

Figure 2. a) Plots of contrast ratios versus Voltage depicting hysteresis. The “coercive” voltage Vc is approximately 0.2V(see text). b) Development of b* during charging slope of b vesus log(t) is 0.53±0.04 for both curves.

A

B

Figure 3. Impedance spectra from ATO EC fresh(left) and yellowed(right) cells. Lines indicate best fit obtained from Zsimp.

Figure 4. X-ray diffraction patterns obtained from fresh, and anodic and cathodic regions of yellowed samples. 110 reflection was fitted to a sum of two Gaussians to obtain peak width and positions.

Figure Y. Mechanism of aging.

# Text boxes

Electrochromic Layer

Dispersion

Metal Oxide

Conductive

Fresh Device

Li+

Electrolyte

ATO

ATO

Gel Electrolyte

Aged Device

Electrolyte

LiSbO3

C Ink

Ag/C Ink

Counter

Electrode

Insulator

Working

Electrode

Polymer Support

## Aged

Device

Device Under

## Test

Untreated

Device